## Slide 1
Application of the TUD-W Benchmark for Nuclear Data and code Validation
Marta Campos Fornés*, Marco Fabbri, Luigino Petrizzi, Aljaz Kolsek, Davide Laghi
8th of April 2025
FUSION NEUTRONICS MEETING:
ITER AND BEYOND

## Slide 2: Outline
Introduction and presentation of the TUD-W SINBAD benchmark
Conversion of the benchmark model: MCNP → OpenMC
Analysis of the neutron spectra results
Analysis of the gamma spectra results
Investigation of discrepancies in high-energy photons
Conclusions and possible future work

## Slide 3: Introduction and presentation of the TUD-W SINBAD benchmark
Objective:
Validation study of tungsten nuclear data across 2 different transport codes.
Description:
Use of the TUD-W SINBAD benchmark, which consists of a thick tungsten alloy block (DENSIMET).
Source employed: almost isotropic emitting around neutrons.
Computation and comparison of spectral neutron and photon flux at four positions in depth: and .
Experimental results (NE 213 scintillation spectrometer) + transport codes (MCNP 6.2, OpenMC 0.15.0).
Weight windows applied for the simulations in positions 2, 3 and 4 (and in depth).
DENSIMET-176
DENSIMET-180
Neutron source

## Slide 4: Conversion of the benchmark model: MCNP OpenMC
Translation of geometry and materials using csg2csg.
Definition of tallies according to the benchmark documentation.
Translation of source using the models uploaded to openmc_fusion_benchmarks (S. Segantin, MIT) as a reference and studying source angular and energy distribution equivalences between MCNP and OpenMC (angular distribution with a specific energy distribution defined for each angular position).
Short scoping study for weight windows performance in OpenMC.
OpenMC verification for a point source collimated into a cone of directions.
DENSIMET-176
DENSIMET-180
Neutron source

## Slide 5: Analysis of the neutron spectra results I
Clear agreement between MCNP and OpenMC results for all 4 positions OpenMC validation.
General agreement between experimental and simulated results, with discrepancies mostly appearing above .

## Slide 6: Analysis of the neutron spectra results II
Exp vs MCNP (FENDL 3.2c, FENDL 3.1d, FENDL 2.1, ENDFB VIII.0)

## Slide 7: Analysis of the neutron spectra results III
Exp vs MCNP (FENDL 3.2c) vs OpenMC (FENDL 3.2c)
Notes: Agreement between different transport codes ⇒ discrepancies driven by the nuclear data.

## Slide 8: Analysis of the photon spectra results I
Clear agreement between MCNP and OpenMC results for all 4 positions OpenMC validation.
Significant deviations in several peaks above . Posterior investigation on the origin of these peaks and the cause of the deviation.

## Slide 9: Analysis of the photon spectra results II
Exp vs MCNP (FENDL 3.2c, FENDL 3.1d, FENDL 2.1, ENDFB VIII.0)
Exp vs MCNP (FENDL 3.2c) vs OpenMC (FENDL 3.2c)

## Slide 10: Investigation of discrepancies in high-energy photons
MCNP PKMT card employed to enable gamma production for different elements.
~ line originated from reactions.
Highest energy peaks resulting from and , impurities present in DENSIMET.
Critical role of impurities in prompt radiation transport, not only in activation studies.
Clear need to characterize and certificate materials to ensure accurate response predictions.

## Slide 11: Conclusions and possible future work
Key outcomes:
Validation of the tungsten nuclear data using the TUD-W SINBAD experiment and 2 different transport codes (MCNP 6.2 & OpenMC 0.15.0).
General underestimation for high-energy photons responses.
Conversion of the TUD-W experimental benchmark model to OpenMC format with a special focus on the source transformation.
Validation of the OpenMC transport code for this case.
Better understanding of OpenMC weight windows efficacy.
Benchmark added to JADE
Possible future work:
Scoping studies to assess whether impurity levels are consistent with the material certificate.
Understand the importance of the different reaction channels.
DENSIMET-176
DENSIMET-180
Neutron source

## Slide 12: Thank you for your attention
Follow us on:
www.f4e.europa.eu
www.twitter.com/fusionforenergy
www.youtube.com/fusionforenergy
www.linkedin.com/company/fusion-for-energy www.flickr.com/photos/fusionforenergy