## Slide 1: Photoneutron activation of the primary cooling circuit of the Hylife-II reactor
F. Ogando, TECF3IR-UNED

## Slide 2: Outline
Background: the Hylife-II reactor.
Activation of the breeder fluid.
Neutron production and activation along the cooling circuit.

## Slide 3: An IFE reactor concept: Hylife-II
Thick wet-wall IFE reactor by R.W. Moir in 1993.
Three layers of liquid flibe:
  Jet array for neutron and Xray absorption. Receives very high neutron fluence.
  Spray for clearing and Xray protection
  Blanket for enhanced TBR.
working on advanced Hylife-III design

## Slide 4: Hylife-II chamber main parameters
Table shows parameters for the 3-chamber design (case B).
Fusion power: 945 MW.
Breeder fluid: FLiBe
  Low density (pumping power)
  Good TBR values.
  Also has downsides, like anything else…
Magnitude | Value
Fusion yield | 350 MJ
Energy multiplication | 1.15
Repetition rate | 2.7 Hz
Chamber radius | 3 m
Flibe flow rate | 34.43 m3/s total 32.37 m3/s jet array
Flibe inventory | 250 m3
IHX flow fraction | 6%
Jet residence time | 0.4 s
Spray residence time | 3 s
Cooling pipe diameter | 60 cm

## Slide 5: Fible flow topology
Chamber
HX
A4
Separate blanket and jet flows
Sump

## Slide 6: Activation levels in equilibrium (after ∞ loops)
Activities (GBq/cm3) | N-16 | F-20 | F-18
a(1) Pre-chamber | 31 | 1.7 | 10.5
a(4) Post chamber | 67 | 2.8 | 10.5
Chamber
HX
A1
A4
Additional TBR | ~ 10-5
Dose Neutrons @ 30cm | 50 Sv/h
Dose Photons @ 30cm | 10.000 Sv/h
Neutron flux in pipe | 2·108 n/cm2/s
Consideration of average fluxes. Peak pulses at x2 in N16 & F20
94%
t=7s
6%
t=21s

## Slide 7: Photonuclear reactions
Data from TENDL19
Decay gamma energies

## Slide 8: Neutron fluxes in cooling pipes
Photon source: ~7·1010 ph/cm3/s
Neutrons /photon = ~2·10-4
  <E> = 1.54 MeV.
  2% from Be multiplication.
Flux in SS304 pipe: 3·108 n/cm2/s
  Semi infinite Contact Dose after 5yr: ~1 mSv/h.
  Actual doses @1m ~150 µSv/h
  Responsible: Co58 from Ni, Co60 from Co, Mn-54 from Fe.
ø60cm
Thick: 0.5”

## Slide 9: Is this relevant? Relatively.
A. Klix, “Activation of Flibe with 14 MeV DT neutrons”
Flibe activity decays rapidly after shutdown.
Doses from FLiBe still dominate doses over pipes over years.
Pipes will dominate after FLiBe drainage.
Waste consideration.

## Slide 10: Conclusions
Thick wet-wall IFE reactors are an attractive technological option
  Xcimer Energy Corporation is evolving this concept.
FLiBe is used as breeding fluid and becomes very active after receiving fusion neutrons.
  Largest activity from: N-16, F-20 and F-18 (all coming from fluorine).
Decay gammas trigger photonuclear reactions in beryllium, producing neutrons and activating the cooling circuit.
  May result in impurity limitation in steels.
This phenomenon can be better studied with tools like FLUNED considering realistic CFD.