## Slide 1
Fusion Neutronics Meeting 2025, 7th-10th April, 2025 Facultad de Educación of UNED, Madrid
N. Fonnesu
ENEA, Nuclear Department, Frascati, Rome
nicola.fonnesu@enea.it
Neutronic benchmark and validation experiments at the Frascati Neutron Generator

## Slide 2
Introduction
Frascati Neutron Generator (FNG)
Electrostatic accelerator-driven neutron source
D+ ions (10 µA-1.25 mA) are accelerated up to ~ 300 keV onto a tritiated target where neutron are produced by means of nuclear fusion reactions
Neutron yield rate range= 108 - 1.5x1011 n/s
Max n flux ~ 5x109 cm-2s-1 @ 14 MeV, ~ 5x107 cm-2s-1 @2.5 MeV
Maximum fluence ~ 1014 cm-2 @ 14 MeV (25 hours @ full power, limit due to target depletion)
2025 Fusion-relevant experiments at FNG
In line with its role in Fusion, three main experiments devoted to benchmark and validation (of some computational methods, codes and nuclear data) and electronics testing are foreseen at FNG in 2025, focused on:
Activated corrosion products (ACPs)
Shielding properties of concrete
GENeuSIS assembly
S. Noce presentation
R. Villari, M. Damiano presentations

## Slide 3
ACP loop at FNG
Corrosion, erosion and release phenomena play an important role in mobilizing activated materials in fusion machines.
ACPs are a concern in terms of occupational radiation exposure (ORE).
The reference code for the ACPs assessment in ITER framework is OSCAR-Fusion developed by CEA.
Experimental validation of ACP codes are mainly in Fission, validation experiments are needed in Fusion.
Design experiments at the Frascati Neutron Generator (FNG) under ITER relevant conditions to validate the OSCAR-Fusion code and methodology for ITER assessment of radiation field due to ACP.
Aim is reproducing thermo-hydraulic (water temperature, velocity, Reynolds number), chemical (pH, oxygen content) and neutronic conditions relevant for ITER in a water circuit at a smaller scale by exploiting hydraulic similarity as much as possible considering laboratory and safety constraints.
OSCAR models which can be explored at FNG
Deposition (Particles)
Dissolution-Precipitation (Ions and particles)
Fluid-dynamics transport & purification (Ions and particles)
Corrosion/Erosion -> Experiment at RINA labs. on Cu samples in autoclave in reducing environment (240°C, 45 bar, O2 < 10 ppb)

## Slide 4: ACP loop at FNG - Final Layout
LiOH/KOH: pHT= 7
Filtering branch:
1- µm Polypropylene
mixed bed resins
N2 line to:
-pressurize (6 bar)
- Keep O2 @ 10 ppb
Measurement of Bq/cm3
γ emitters detection
Measurement of Bq/cm2
γ emitters detection
Injection point (solid particles, ions)
Heating and pumping unit (140°C, 6 bar)

## Slide 5
Study of pipe deposit formation depending on:
Material impact: one SS316L line and one Cu line
Rugosity: 0.5 and 10-µm pipes in the same line
Fluid-dynamics: effect of turbulence due to flow area change
Cu
SS316L
ACP loop at FNG - Final Layout

## Slide 6
Comparison of water conditions ACP loop at FNG vs. ITER IBED
The relevancy for ITER case is confirmed by comparison with typical water conditions expected in the ITER IBED PHTS during plasma operation of the tokamak, i.e., water temperature =150°C, velocity 10 m/s, Reynolds number 106-107, water pHT =7 and the capability of reproducing low O2 content in water (10 ppb) up to natural concentration.
Parameter | ACP loop | ITER IBED PHTS during plasma operation
Water type | Demineralized water | Demineralized water
Nominal Temperature and Pressure | 140°C, 6 bar | 150°C, 40 bar
Maximum Volumetric Flow Rate | 80 l/min | 
Nominal Volumetric Flow Rate | 60 l/min | 
Maximum water speed | 15 m/s | 
Linear length of the loop | 20 m | 
Water volume | 20 l | 
Water velocity range | 3-13 m/s | 10 m/s
Reynolds number range | 5x104 – 5x105 | 106 - 107
Oxygen content into the water | 10 ppb – natural concentration | 10 ppb
pHT of water | 7 | 7

## Slide 7: Expected activity at the meas. section, 1g of Cu dust, 1 um
Injection of ACPs into the loop
Surface activity to be measured with HPGe portable spectrometers

## Slide 8: Expected activity at the meas. section, 1g of Cu dust, 1 um
Activity concentration in sampled water to be measured at the well-type HPGe of the lab.
>120 Bq/g

## Slide 9: Concrete shielding benchmark experiment
To improve accuracy in modeling radiation transport for shielding design, some experimental campaigns with ordinary and heavy concrete are planned at FNG, within EUROfusion WP BB.
The DEMO-relevant ordinary concrete shielding benchmark experiment is foreseen in 2025, with a mock-up consisting of thirty-six 50x50x5 cm3 slabs of ordinary concrete, its feasibility being demonstrated by a thorough MCNP pre-analysis with JEFF 3.3 and IRDFF 2 data libraries, respectively for transport and dosimetry.

## Slide 10: Concrete shielding benchmark experiment
D. Flammini, Conceptual layout of a DEMO relevant concrete shielding benchmark experiment (ENEA), WPBB-S.05.02-T008-D003, EUROfusion Report
The pre-analyses defined the experimental configuration for to have both measurable activated foils and low background (< 10%) due to scattered neutrons, so that the experimental response of the detectors is a measure of the neutron transport inside the concrete mock-up and it is not influenced in a significant way by the surrounding environment.

## Slide 11: Silica-based optical fibers for 14 MeV neutron beam monitoring
Luca Weninger et al., Potential of radioluminescent silica-based optical fibers for 14 MeV neutron beam monitoring, Results in Optics 19 (2025) 100807
Ce-doped optical fibers, based on the radiation-induced luminescence (RIL) phenomenon RIL response calibrated to the neutron flux, via a linear fit between the facility monitors and the optical fiber response.

## Slide 12: Silica-based optical fibers for 14 MeV neutron beam monitoring
Luca Weninger et al., Potential of radioluminescent silica-based optical fibers for 14 MeV neutron beam monitoring, Results in Optics 19 (2025) 100807
Ce-doped optical fibers, based on the radiation-induced luminescence (RIL) phenomenon RIL response calibrated to the neutron flux, via a linear fit between the facility monitors and the optical fiber response.

## Slide 13
Concluding Remarks
ACP loop at FNG
Engineering of the project completed (both hardware and control system)
Installation and test (water chemistry and thermo-hydraulic) by July 2025
A proposal of experiment of Cu dust <=11 g compliant with safety and quality of experiment by 2025
Concrete shielding benchmark experiment
DEMO-relevant ordinary concrete shielding benchmark experiment (36 50x50x5 cm3 slabs) is foreseen in 2025
Feasibility demonstrated by MCNP pre-analysis with JEFF and IRDFF-II data libraries
Neutron flux and fluence will be measured at different depths of penetration both with activation foils and some active detectors, among which, the promising radioluminescent optical fiber developed by Laboratoire Hubert Curien.

## Slide 14
Thank you!
N. Fonnesua, T. Berryb, A. Colangelia, F. Dacquaitc, M. Damianod, D. Flamminia, S. Girarde, X. Litaudonc, D. Leichtlef, S. Loretia, M. Lungaronia, A. Moranae, F. Moroa, S. Nocea,
A. Pietropaoloa, A. Previtia, N. Terranovaa, R. Villaria, L. Weningere, P. Zitoa
EUROfusion Consortium, JET, Culham Science Centre, Abingdon, OX14 3DB, UK
a ENEA, Nuclear Department, Via E. Fermi 45, 00044 Frascati, Rome, Italy
b United Kingdom Atomic Energy Authority, Culham Science Centre, Abingdon, OX14 3DB, UK
c CEA, Cadarache, F-13108 St-Paul-Lez-Durance, France
d University of Rome “Tor Vergata”, Industrial Engineering Department, Via del Politecnico 1, 00133, Rome, Italy
e Laboratoire Hubert Curien, UMR-CNRS 5516, Université Jean Monnet, F-42000 Saint-Etienne, France
g Karlsruhe Institute of Technology, 76344 Eggenstein-Leopoldshafen, Karlsruhe, Germany​
nicola.fonnesu@enea.it

## Slide 15
Element | Weight (%) | 
 | Ordinary Concrete | Heavy Concrete
H | 0.35 | 0.3
C | 10.29 | -
O | 49.66 | 28.6
Na | - | 0.18
Mg | 9.87 | 0.27
Al | 0.75 | 0.69
Si | 1.99 | 2.57
P | - | 0.45
S | 1.07 | 0.13
Cl | 0.02 | 0.01
K | 0.06 | 0.17
Ca | 24.16 | 4.7
Ti | 0.05 | 0.03
Fe | 1.73 | 61.9
Density [g/cm3] | 2.55 | 3.94
Reaction | Half-life | Isotopic abundance (%) | Dominant Ray energy (keV) | Dominant Ray branching (%) | Reaction Threshold (MeV)
27Al(n,a)24Na | 14.96 h | 100.0 | 1368.63 | 100.0 | 4.2
56Fe(n,p)56Mn | 2.58 h | 91.8 | 847 | 98.9 | 3.0
115In(n,n’)115mIn | 4.49 h | 95.7 | 336.24 | 45.9 | 0.5
197Au(n,g)198Au | 2.696 d | 100.0 | 411.80 | 95.6 | -
93Nb(n,2n)92mNb | 10.15 d | 100.0 | 934.53 | 99.0 | 8.9
58Ni(n,p)58Co | 70.82 d | 68.27 | 810.77 | 68.3 | 1.0
58Ni(n,2n)57Ni | 35.60 h | 68.27 | 1377.63 | 81.7 | 12.5
186W(n,g)187W | 23.9 h | 28.6 | 685.75 | 26.4 | -
Reaction | Half-life | Isotopic abundance (%) |  |  | Reaction Threshold (MeV)
27Al(n,a)24Na | 14.96 h | 100.0 | 1368.63 | 100.0 | 4.2
56Fe(n,p)56Mn | 2.58 h | 91.8 | 847 | 98.9 | 3.0
115In(n,n’)115mIn | 4.49 h | 95.7 | 336.24 | 45.9 | 0.5
197Au(n,g)198Au | 2.696 d | 100.0 | 411.80 | 95.6 | -
93Nb(n,2n)92mNb | 10.15 d | 100.0 | 934.53 | 99.0 | 8.9
58Ni(n,p)58Co | 70.82 d | 68.27 | 810.77 | 68.3 | 1.0
58Ni(n,2n)57Ni | 35.60 h | 68.27 | 1377.63 | 81.7 | 12.5
186W(n,g)187W | 23.9 h | 28.6 | 685.75 | 26.4 | -
Spare-1

## Slide 16
Spare-2