## Slide 1: Overview of the Neutronics Calculations for EU DEMO at Lithuanian Energy Insitute
Simona Breidokaitė, Gediminas Stankūnas, Andrius Tidikas
Lithuanian Energy Intitute
April 9, 2025

## Slide 2
Introduction:
2007
2012
2014
LEI signed EFDA association agreement and became involved in FUSION research
Activities mainly devoted to supporting the implementation of W7-X:
  Deterministic safety analysis
  Strength analysis of the port welds
  RAMI assessment
LEI become involved in activities related to neutronics in:
DONES,
DEMO
JET
LEI became a member of FuseNet
EUROfusion project which LEI
JET campaigns:
Bolometric data analysis
Activation and dose rates calculations
SAFETY:
WCLL, HCPB DEMO neutronics calculations
  Deterministic safety analysis
  RAMI assessment
ENS:
Neutronics analysis and SDDR of Hight Flux Test Module (HFTM) and Target Assembly

## Slide 3: Model:
6 pav. WCLL Ličio klojinio MCNP modelis
7 pav. EU DEMO divertoriaus MCNP modelis.
4 pav. Vakuminio indo MCNP modelis
WCLL
HCPB
J.H. You, et all., Divertor of the European DEMO: Engineering and technologies for power exhaust, Fusion Engineering and Design, Volume 175, https://doi.org/10.1016/j.fusengdes.2022.113010
P. Pereslavtsev, et all., Neutronic Activity for Development of the Promising Alternative Water-Cooled DEMO Concepts, Applied Sciences. 13. https://doi.org/10.3390/app13137383
P. Pereslavtsev, et all., Analyses of the shielding options for HCPB DEMO blanket, Fusion Engineering and Design, Volume 156, https://doi.org/10.1016/j.fusengdes.2020.111605.
1
2
3
DEMO Base Line 2017. 11.25° + 2019 DIVERTOR
Homogenized BB
5 semi-Heterogenized components
DEMO Base Line 2017.
Homogenized BB
3 homogenized layers
EU DEMO1 2018
Heterogenized BB
Breeding blanket cells

## Slide 4: Methodology:
MCNP
ADVANTG
Geomtry
Material describtion
Source describtion
Neutron flux
Neutron spectra
Nuclear data laibraries:
FENDL
JEFF
Specific activity
Decay Heat
Dose Rate
Nuclear data libraries
TENDL
FISAPCT-II
Particle transport calculations are performed using the MCNP code based on the Monte Carlo method.
To reduce statistical errors, and at the same time the duration of calculations, the variance reduction tool ADVANTG was used.
The FISPACT-II software package was chosen to be used for the analysis of nuclear reaction products, specific activity and decay heat
1
2
1.1

## Slide 5
Functional materials
Lithium Orthosilicate
Lithium - lead
Water
Constructional materials
Stainless steels (Eurofer ir 316L(N)-IG)
Tungsten alloys (W ir W + CuCrZr+ Water)
Titanium alloy
Nickel-chromium-based superalloy (Inconel)
Reaction products:
1
2
3
1
2
3
4

## Slide 6: Reaction Products:1s
 | Nuclide | Primary reactions | 
Eurofer | 56Mn | 56Mn(n, γ),56Fe(n,p) | 0.4; 88.698
316L(N)-IG | 56Mn | 56Mn(n, γ),56Fe(n,p) | 2: 60
Water | 16N | 16O(n, p) | 88
Tungsten | 187W | 186W(n, γ) | 99.96
W + CuCrZr+ Water | 187W | 186W (n, γ) | 81.9957
Ti alloy | 52V | 51V(n, γ) | 4.5
Inconel | 182Ta | 181Ta(n, γ) | 5.175
Lithium orthosilicate | 16N, | 16O(n,p) | 50
Li-Pb | 207Pb | 208Pb(n, γ) | 99.45

## Slide 7: Reaction Products: 100y
 | Nuclide | Primary reaction | 
Eurofer | 14C | 14C(n,p) | 0.11
316L(N)-IG | 14C | 14C(n,p) | 0.028
Water | 14C | 17O(n,α) | 88
Tungsten | 91Nb, 108mAg | 192Mo(n,2n) 109Ag(n,2n) | 0.01; 0.001
W + CuCrZr+ Water | 63Ni | 63Cu(n,p) | 15.02
Ti alloy | 14C | 14C(n,p)17O(n,α) | 0.28: 0.2
Inconel | 94Nb | 93Nb(n, γ) | 5.125
Lithium orthosilicate | 14C | 17O(n,α) | 50
Li-Pb | 203Pb | 204Pb(n,2n) | 99.45

## Slide 8: Breeding blanket impact:
Was Evaluated:
Neutron Flux/Spectra
Specific Activity
Decay Heat
1
2
3

## Slide 9: Breeding Blanket
Y=122
At first wall
Neutron flux- 1.18 (WCLL)
Doee rate– 1.16 (WCLL)
Breeding zone:
Neutron flux- 2.43 (WCLL)
Dose rate– 2 (WCLL)
Back Suppor system:
Neutron flux– 5.34 (HCPB)
Dose rate–8.55 (HCPB)
1
2
3
Ratio:

## Slide 10: Breeding materials
Specific Activity – 1.79
Decay Heat – 0.57
Specific Activity - 10
Decay Heat – 6
Specific Activity – 0.19
Decay Heat – 0.24
1s
10 metai
100 metų
1
2
3
4
28Al half life: 2.24 min
203Pb half life: 2.16 d
45Ca half life: 162.61 m
204Tl half life: 3.77 m

## Slide 11: Vacuum vessel
44 pav. . Neutronu spektras vakuuminiame inde
Neutron flux:
In energy groups between (10-7- 0.4 MeV) – 10
In energy groups between (0.4- 15 MeV) – 5
Specific Activity: (HCPB/WCLL ratio)
Inner – 5
Interspace – 9.31
Outer – 1.71
Decay heat:
Inner – 2.73
Interspace – 9.25
Outer – 3.35
1
2
3
Ratio:

## Slide 12: Divertor
WCLL/HCPB: 1.17
WCLL/HCPB: 1.46
WCLL/HCPB: 1.10
Inboard upper
Middle upper
Middle bottom

## Slide 13
Deacy heat: 1,19
Specific Activity: 1,17
Decay Heat: 1,23
Specific Activity: 1,09
Decay heat: 1.02
Specific Activity: 1.22
1s.
1 year
100 years
WCLL/HCPB ratio:

## Slide 14: Materials radioactive waste classification
Intermediate-level waste (ILW)
High level waste(HLW)
Low-Level Waste(LLW)
Acceptance criteria
<1.6 × 10⁷ Bq/kg
Acceptance criteria
<2 kW/m³
World nuclear associate (WNA)

## Slide 15
Vacuum vessel (Inner and Interpsace)
Divertor componenst (except WH)
First second
Vacuum Vessel (Outer shell)
Breeding materials
Wishbone (Inconel)
Divertor: 176 GBq/kg- 756 TBq/kg
Breeding Blanket: 5.03 TBq/kg – 16 TBq/kg
Vacuum vessel: 14.4 GBq/kg – 5,26 GBq/kg
0.3 kW/m3 - 1430 kW/m3
1 W/m3 - 180 kW/m3
1 W/m3 – 11 W/m3
Intermediate Level Waste(ILW)
High Level Waste(HLW)
Low Level Waste (LLW)
Acceptance criteria
<1.6 × 10⁷ Bq/kg
Acceptance criteria
<2 kW/m³
1
2
3

## Slide 16
Divertor: 0.373 GBq/kg-13.9 TBq/kg
Breeding blanket: 0.26 GBq/kg – 13.4 GBq/kg
Vacuum vessel: 1.54 GBq/kg – 0.381 TBq/kg
All components
After 1 year
2.94 mW/m3 – 1.28 kW/m3
0.751 W/m3 – 0.3 kW/m3
10.2 µW/m3 – 1.3 mW/m3
Intermediate Level Waste(ILW)
High Level Waste (HLW)
Low Level Waste(LLW)
Acceptance criteria
<1.6 × 10⁷ Bq/kg
Acceptance criteria
<2 kW/m³
1
2
3

## Slide 17
Divertor: 0.35 MBq/kg-13 GBq/kg
Breeding Blanket: 34.7 MBq/kg – 13.7 GBq/kg
Vacuum vessel: 34.7 MBq/kg – 13.7MBq/kg
After 100 years
12.1µW/m3 – 0.336 W/m3
0.77 mW/m3 – 0.336 W/m3
6.26 nW/m3 – 0.145 µW/m3
Ti Alloy
Tungsten in PFC
Rest divertor components
Breeding materials
Vacuum vessel
1
2
3
Intermediate Level Waste(ILW)
High Level Waste (HLW)
Low Level Waste(LLW)
Acceptance criteria
<1.6 × 10⁷ Bq/kg
Acceptance criteria
<2 kW/m³

## Slide 18: Thank you for your attention 