## Slide 1: Activation Analysis on the DEMO Divertor Materials: study of the impact of chemical composition and operational scenario
Author: M. Lungaronia
Contributors: S. Nocea, N. Fonnesua, A. Colangelia, D. Flamminia, F. Moroa, A. Previtia,
G. Mazzonea, S. Roccellaa, J.H Youb and R. Villaria
aENEA NUClear Department
bMax-Planck-Institut
Neutronics Meeting – 6/11 April 2025, Madrid

## Slide 2
Summary
Introduction & Background:
  DEMO Divertor MCNP Model
Full Activation Analysis:
  Neutronic Spectra
  Irradiation & Cooling History
  Materials
  Specific Activity
  Contact γ-Dose Rate
Sensitivity Analysis:
  Impurities on CuCrZr
  Impurities on SS316Ti
  Conclusion

## Slide 3: Nuclear Analysis: Modelling
2022 DIV Double-coolant concept integrated in WCLL DEMO with target supports made of SS316-Ti
CAD
MCNP
3D MCNP model
The study of the activation of the In-vessel components materials and the related impact of impurities represent a fundamental element for the design and waste management of future fusion machines such as DEMO
Pfus 1998 MW =7.1x1020 n/s
EFDA_D_2PPMQB
Three-dimensional neutronics analysis with MCNP5.1 Monte Carlo code & JEFF3.3 nuclear data library:
  Neutron flux & spectra, in all divertor components
Activation analysis with FISPACT-II and TENDL-2017 complete inventory
    Specific Activity, Contact γ-Dose Rate and Decay Heat (in spare slides) for each sub-component
WCLL DEMO model based on 2017 Generic DEMO

## Slide 4: Full Activation Analysis: Neutron spectra calculations
For the Full Activation Analysis 27 energy neutron spectra were calculated using MCNP5.1.
inputs for FISPACT inventory calculations.
Spectrum # | Components Name | Total Fluxes [n/cm2s]
1 | Cassette Body - EUROFER | 2,12E+13
2 | OB fix system VV + bridge - EUROFER | 3,29E+12
3 | Pumping Shield - SS316LN-(IG) | 2,78E+12
4 | IB fix system VV - EUROFER | 2,78E+12
5 | PF coil structure - EUROFER | 4,09E+12
6 | PF coil conductor - Pure Cu | 4,02E+12
7 | PFC cooling system - SS316Ti | 1,03E+13
8 | IB target - CB fix system - Inconel 718 | 4,95E+13
9 | OB target - CB fix system - Inconel 718 | 4,14E+13
10 | PFC - 1st layer - Tungsten | 2,94E+14
11 | PFC - 2nd layer - CuCrZr | 2,52E+14
12 | PFC - 3rd layer - Tungsten | 2,28E+14
13 | PFC - 4th layer EUROFER | 2,20E+14
14 | Inboard target - SS316Ti | 1,41E+14
15 | Liner - EUROFER | 1,64E+14
16 | Liner - II layer EUROFER + Water | 4,13E+14
17 | Liner - Tungsten (1st layer) | 4,06E+14
18 | Reflector plates OB - Tungsten (1st layer) | 1,86E+14
19 | Reflector plates IB - Tungsten (1st layer) | 2,48E+14
20 | Neutron shielding - EUROFER | 2,16E+13
21 | Outboard target - SS316Ti | 1,05E+14
22 | Inboard Reflector plate - EUROFER | 1,92E+14
23 | Outb Reflector plate - EUROFER | 1,49E+14
24 | Reflector plates' connecting pipes - EUROFER | 7,87E+13
25 | PFC-target connecting pipes - CuCrZr | 9,36E+13
26 | TGs feeding pipes - EUROFER | 9,45E+12
27 | Wishbone - Ti6Al4V | 5,07E+12
Nine components are selected to represent the others
A Full Activation Radwaste Inventory has been performed

## Slide 5: Full Activation Analysis: Irradiation & Cooling History
Irradiation scenario equivalent to 1.57 FPY
continuous operation phase over 5.2 years (CY) minus 10 days at 30% of the nominal fusion power
10 days pulsed operation with 48 pulses of 4 hours at full power & 1 hour dwell time
EFDA_D_2L8TR9
Cooling Time
16 specific cooling times have been selected
In particular, the cooling time used are:
1 s
10 s
1 min
1 h
1 d
7 d
12 d
30 d
90 d
1 y
5 y
10 y
30 y
100 y
1000 y
10000 y

## Slide 6: Full Activation Analysis: Materials
CuCrZr |  | SS316LN-IG |  | EUROFER |  | SS316Ti |  | Inconel 718 |  | W |  | Ti6Al4V |  | Pure Cu | 
Density | 8,9 | Density | 7,93 | Density | 7,87 | Density | 7,93 | Density | 8,221 | Density | 19,00 | Density | 4,421 | Density | 8,96
Cu | 98,710 | Fe | 63,684 | Fe | 88,698 | Fe | 63,923 | C | 0,08 | W | 99,9595 | Ti | 88,0075 | Co | 0,05
Cr | 0,750 | C | 0,03 | C | 0,110 | C | 0,08 | Mn | 0,35 | Ag | 0,001 | Al | 6,75 | Ta | 0,01
Zr | 0,110 | Mn | 2 | Mn | 0,4 | Mn | 2 | Si | 0,35 | Al | 0,0015 | V | 4,5 | Nb | 0,1
Co | 0,050 | Si | 0,5 | Cr | 9 | Si | 0,75 | P | 0,015 | As | 0,0005 | Fe | 0,4 | Cu | 99,84
Ta | 0,010 | P | 0,025 | V | 0,2 | P | 0,045 | Si | 0,015 | Ba | 0,0005 | O | 0,2 | Sum | 100
Nb | 0,100 | S | 0,01 | Ta | 0,12 | S | 0,03 | Cr | 19 | Ca | 0,0005 | C | 0,08 |  | 
B | 0,001 | Cr | 18 | W | 1,1 | Cr | 17 | Nb | 5,125 | Cd | 0,0005 | H | 0,0125 |  | 
O | 0,032 | Ni | 12,5 | N | 0,03 | Ni | 12 | Ta | 5,175 | Co | 0,001 | N | 0,05 |  | 
Mg | 0,04 | Mo | 2,7 | Ti | 0,02 | Mo | 2,5 | Co | 1 | Cr | 0,002 | Sum | 100 |  | 
Al | 0,003 | N | 0,08 | P | 0,005 | N | 0,1 | Mo | 3,05 | Cu | 0,001 |  |  |  | 
Si | 0,04 | B | 0,001 | Si | 0,05 | B | 0,002 | Fe | 11,634 | Fe | 0,003 |  |  |  | 
P | 0,014 | Cu | 0,3 | S | 0,005 | Cu | 1 | Al | 0,5 | K | 0,001 |  |  |  | 
S | 0,004 | Co | 0,05 | Ni | 0,01 | Co | 0,05 | Ti | 0,9 | Mg | 0,0005 |  |  |  | 
Mn | 0,002 | Nb | 0,01 | Mo | 0,005 | Nb | 0,01 | Ni | 52,5 | Mn | 0,0005 |  |  |  | 
Fe | 0,02 | Ti | 0,1 | Cu | 0,01 | Ti | 0,5 | B | 0,006 | Na | 0,001 |  |  |  | 
Ni | 0,06 | Ta | 0,01 | Nb | 0,005 | Ta | 0,01 | Cu | 0,3 | Nb | 0,001 |  |  |  | 
Zn | 0,01 | Sum | 100 | Al | 0,01 | Sum | 100 | Sum | 100 | Ni | 0,0005 |  |  |  | 
As | 0,01 |  |  | B | 0,002 |  |  |  |  | Pb | 0,0005 |  |  |  | 
Sn | 0,01 |  |  | Co | 0,01 |  |  |  |  | Ta | 0,002 |  |  |  | 
Sb | 0,011 |  |  | As | 0,05 |  |  |  |  | Ti | 0,0005 |  |  |  | 
Pb | 0,01 |  |  | Sn | 0,05 |  |  |  |  | Zn | 0,0005 |  |  |  | 
Bi | 0,003 |  |  | Sb | 0,05 |  |  |  |  | Zr | 0,0005 |  |  |  | 
Sum | 100 |  |  | Zr | 0,05 |  |  |  |  | Mo | 0,01 |  |  |  | 
 |  |  |  | O | 0,01 |  |  |  |  | C | 0,003 |  |  |  | 
 |  |  |  | Sum | 100 |  |  |  |  | H | 0,0005 |  |  |  | 
 |  |  |  |  |  |  |  |  |  | N | 0,0005 |  |  |  | 
 |  |  |  |  |  |  |  |  |  | O | 0,002 |  |  |  | 
 |  |  |  |  |  |  |  |  |  | P | 0,002 |  |  |  | 
 |  |  |  |  |  |  |  |  |  | S | 0,0005 |  |  |  | 
 |  |  |  |  |  |  |  |  |  | Si | 0,002 |  |  |  | 
 |  |  |  |  |  |  |  |  |  | Sum | 100 |  |  |  | 
Materials Chemical composition with impurities
  The complete inventory after shutdown have has been assessed with FISPACT.
  Graphs on temporal evolution of:
    Specific Activity
    Contact γ-Dose Rate
    Decay Heat (in spare)
Ref:
EUROfusion -> EFDA_D_2MM3A6
ITER -> ITER_D_HTN8X3, ITER_D_REYV5V
* -> ASME Boiler and Pressure Vessel Code An International Code + missing impurities coming from SS 316L(N) steel (X2CrNiMo17-12-2 controlled nitrogen content) ref EFDA_2MM3A6 + increased Ti content according to G. Mazzone, 0.5%
Ref
EUROfusion
Ref
EUROfusion
Ref
EUROfusion
Ref
ITER
Ref
ITER
Ref
EUROfusion
Ref
ITER
Ref
*

## Slide 7: Full Activation Analysis: Specific Activity
9 main DIV components
T < 1 day
CuCrZr activity is higher than Eurofer, SS316Ti and Inconel 718.
2 day < T < 10 year
The activity of Eurofer and Inconel 718 has relevant and quite constant. The activity of CuCrZr falls below the Eurofer.
T > 10 year
The activity of Eurofer and W collapses while SS316Ti, Inconel 718 and CuCrZr remain predominant.

## Slide 8: Full Activation Analysis: Contact γ-Dose Rate
T < 1 day
The contact dose rate of Eurofer, W and Inconel 718 is higher than SS316Ti and Ti-alloy.
2 day < T < 10 year
The contact dose rate of W is the lowest together with Ti-alloy. The dose of Inconel 718 remain predominant, followed by CuCrZr.
T > 10 year
The trend is quite similar all materials. The higher contact γ- dose is Inconel 718.
9 main DIV components

## Slide 9: Sensitivity Analysis: Impurities on CuCrZr
Impurities concentration of CuCrZr |  |  |  |  |  |  | 
%wt | CuCrZr 0 | CuCrZr 1 | CuCrZr 2 | CuCrZr 3 | CuCrZr 4 | CuCrZr 5 | CuCrZr 6
Cu (Balance) | 98,71 | 98,870 | 98,854 | 98,838 | 98,790 | 98,550 | 98,805
Co | 0,05 | 0 | 0,005 | 0,01 | 0,025 | 0,1 | 0,05
Ta | 0,01 | 0 | 0,001 | 0,002 | 0,005 | 0,02 | 0,01
Nb | 0,1 | 0 | 0,01 | 0,02 | 0,05 | 0,2 | 0,005
Seven concentration variants of impurities (Co, Ta and Nb) on CuCrZr were analysed (as report in table) using the neutron spectra of PFC - 2nd layer CuCrZr:
Case 0: References Concentration
Case 1: No Impurities
Case 2/5: Impurities Concentration (ref / 10); (ref / 5); (ref / 2); (ref x 2)
Case 6: Co = %wt ref; Ta = %wt ref; Nb = %wt (ref /20)
T < 1 day
There are no appreciable differences, either in activity or in dose.
2 day < T < 30 year
The activity and dose of Co60 is predominates and appreciable
T > 100 year
The activity and dose of Nb94 is predominates and more appreciable the differences
9.5E-3 Sv/h
2.5E-4 Sv/h
3.3E+5 Bq
1.6E+7 Bq
133 Sv/h
281 Sv/h
2.7E+11 Bq
5.3E+11 Bq

## Slide 10: Sensitivity Analysis: Impurities on SS316Ti
Impurities concentration of SS316Ti |  |  |  |  |  | 
%wt | SS316Ti 0 | SS316Ti 1 | SS316Ti 2 | SS316Ti 3 | SS316Ti 4 | SS316Ti 5
Fe (Balance) | 63,923 | 63,993 | 63,932 | 63,853 | 63,958 | 64,173
Co | 0,05 | 0 | 0,05 | 0,1 | 0,025 | 0,05
Ta | 0,01 | 0 | 0,001 | 0,02 | 0,005 | 0,01
Nb | 0,01 | 0 | 0,01 | 0,02 | 0,005 | 0,01
Ti | 0,5 | 0,5 | 0,5 | 0,5 | 0,5 | 0,25
Six concentration variants of impurities (Co, Ta and Nb) on SS316Ti were analysed (as report in table) using the neutron spectra of Inboard Target:
Case 0: References Concentration
Case 1: No Impurities; Ti = %wt ref
Case 2: Co = %wt ref; Ta = %wt ref; Nb = %wt (ref / 10)
Case 3/4: Impurities Concentration (ref x 2); (ref / 2); Ti = %wt ref
Case 5: Co = %wt ref; Ta = %wt ref; Nb = %wt ref; Ti = %wt (ref /2)
T < 1 hour
There are no appreciable differences in dose, but some small differences in activity due to Mn56.
T > 1 hour
The activity presents extremely small differences; while the dose due to Co60, Mn54 Mn56 and Ta182 determine a widespread trend of the Contact γ-Dose Rate
The change in %wt of Ti has no effect on the radwaste inventory
127 Sv/h
21 Sv/h
0.14 Sv/h
3.5 Sv/h
178 Sv/h
336 Sv/h
1.1E+11 Bq
1.9E+11 Bq
3.4E+12 Bq
3.7E+12 Bq

## Slide 11: Conclusions
From the analysis carried out on the main components of the DEMO Divertor, we can conclude that:
  For a short cooling time (less than a month) Tungsten and CuCrZr components have the highest activity. In the intermediate cooling time (between a month and few years) the activity of Eurofer and Inconel 718 become predominant. For a long cooling time (over 100 years) SS316Ti and Inconel 718 materials have the highest activities.
  For a short cooling time (less than a month) Eurofer and Inconel 718 components have the highest contact dose rate. In the intermediate cooling time (between a month and few years) the contact dose rate of CuCrZr overtakes the Eurofer and SS316Ti components. For a long cooling time (over 100 years) the Inconel 718 materials have always the highest Contact γ-Dose Rate, following by the CuCrZr and Eurofer.
  A sensitivity study on Co, Ta and Nb impurities was performed for CuCrZr and SS316Ti. Impurities have a strong impact on the Contact γ-Dose Rate (such as for the SS316Ti, 21 Sv/h vs. 178 Sv/h in the case of no impurities and the double of reference impurities one years after the plasma shutdown) and much less on the Specific Activity values (almost always of the same order of magnitude both for CuCrZr and SS316Ti).
  The change in %wt of Ti in SS316Ti has no effect on the radwaste inventory

## Slide 12
Thanks for your attention

## Slide 13: Nuclear Analysis: Nuclear Heating
Nuclear heating density
Max in the liner: 31 W/cm3 on W layer and 11 W/cm3 on Eurofer
Nuclear heating density on CB-PFU attachments are in the range of 0.45 – 1.58 W/ Max in IVT links & pins - Upper system
Nuclear Heating density in Eurofer components
Total Nuclear power 48 cassette 179.61 MW
18% on the CB & neutron shielding plates
~ 26.6 MW on steel
~ 6.8 MW on water
34% on the PFU
~ 54.8 MW on PFC and structure
~ 6.3 MW on water
42% on the liner
~ 55.4 MW on armour and structure
~ 20.4 MW on water
5% on reflector plates
~ 6.4 MW on armour and structure
~1.3 MW on water
Input for thermal analysis

## Slide 14: Nuclear Analysis: Nuclear Damage
Damage in Eurofer 0.01 – 5.5 dpa/FPY.
On baffle regions of IB&OB target supports and on the top of the liner >4 dpa/FPY
Max in the Eurofer layer below the W-armour in the liner: 5.2 dpa/FPY
The peak damage in the wishbone is ~ 0.1 dpa/FPY.
Peak values higher than 5 dpa/FPY in PFC target support
Max damage in CB-fixation system 0.75 dpa: Inconel- IVT links & pins –upper system
Good shielding performances: cumulated damage on VV < 2.75 dpa over 30 FPY
Hotspots close to Cassettes gaps and other penetrations

## Slide 15: Nuclear Analysis: Gas Production
The H production is generally higher than the He-production.
Max H production 160 appm/FPY & He production 135 appm/FPY in Eurofer - second layer of the liner.
Peak value on the target supports: He 110 appm/FPY and H 170 appm/FPY
The He-concentration on the PFC cooling pipes-targets connection points is exceeded for cutting/re-welding

## Slide 16: Full Activation Analysis: Decay Heat
T < 1 day
The decay heat of CuCrZr is higher in the first minutes than Eurofer (of PFCs), Inconel 718 and W. Lower we find the Eurofer of CB and Ti-alloy.
2 day < T < 10 year
The decay heat of W fall below, while the trend of other materials are similar.
T > 10 year
The decay heat of Inconel 718 is higher of the others, followed by CuCrZr, SS316Ti and Eurofer.
9 main DIV components

## Slide 17: Neutron flux: DIV 2022 + SS316Ti PFC target support
N flux @1998 MW
Neutron flux in divertor components in the range: ~4x1014 n/cm2/s in PFC - 3x1011 n/cm2/s at the IB side close to attachment
Mitigation of the streaming from blanket–divertor gaps, pumping duct and lower port thanks to the implementation of the neutron insert, liner, reflector plates, bridge, and lower port shielding.
Shielding effectiveness of the neutron shield inserts located below the liner well evident in the central and outboard zone

## Slide 18: Sensitivity Analysis: Impurities on CuCrZr & SS316Ti
T < 1 hour
There are no appreciable differences in decay heat.
1 hour < T < 100 year
The decay heat of CuCrZr shown small differences in relation to impurities; while the decay heat of SS316Ti have a widespread trend due to Mn56 and Co60.
T > 100 years
The decay heat in CuCrZr have a large widespread due to Cu62, Cu66 and Co60. In SS316Ti the decay heat is quite constant even when the impurity amounts change.
Impurities concentration of CuCrZr |  |  |  |  |  |  | 
%wt | CuCrZr 0 | CuCrZr 1 | CuCrZr 2 | CuCrZr 3 | CuCrZr 4 | CuCrZr 5 | CuCrZr 6
Cu (Balance) | 98,71 | 98,870 | 98,854 | 98,838 | 98,790 | 98,550 | 98,805
Co | 0,05 | 0 | 0,005 | 0,01 | 0,025 | 0,1 | 0,05
Ta | 0,01 | 0 | 0,001 | 0,002 | 0,005 | 0,02 | 0,01
Nb | 0,1 | 0 | 0,01 | 0,02 | 0,05 | 0,2 | 0,005
Impurities concentration of SS316Ti |  |  |  |  |  | 
%wt | SS316Ti 0 | SS316Ti 1 | SS316Ti 2 | SS316Ti 3 | SS316Ti 4 | SS316Ti 5
Fe (Balance) | 63,923 | 63,993 | 63,932 | 63,853 | 63,958 | 64,173
Co | 0,05 | 0 | 0,05 | 0,1 | 0,025 | 0,05
Ta | 0,01 | 0 | 0,001 | 0,02 | 0,005 | 0,01
Nb | 0,01 | 0 | 0,01 | 0,02 | 0,005 | 0,01
Ti | 0,5 | 0,5 | 0,5 | 0,5 | 0,5 | 0,25